## Slide 1: Updated dilute CV-SANS results
Bailee Barrett
February 02, 2022
Zhang Research Group

## Slide 2: General overview of singly charged peptoid library
General structure of singly charged peptoid
Schematic of singly charged peptoid chains:
Where:
=
=
=
Density: 0.95 g/mL
Density: 1.00 g/mL
Density: 1.00 g/mL
Overall density of peptoid: 0.99 g/mL
Sequence 3 (S3)
Sequence 1 (S1)
Sequence 5 (S5)

## Slide 3: Sequence one
2022 data
(with thermal annealing)
2019 data

## Slide 4: Sequence three
2022 data
(with thermal annealing)
2019 data

## Slide 5: Sequence five
2022 data
(with thermal annealing)
2019 data

## Slide 6: Comparison of all sequences

## Slide 7: Comparison of each contrast
100% D2O
95% D2O
90% D2O

## Slide 8: Comparison of each contrast
85% D2O
80% D2O
75% D2O

## Slide 9
Chemical structure without counter ion:
Molecular Weight: 3361.29 g/mol
Molecular Formula: C162H297N26O47
Number of labile protons in single surfactant: Zero
Molecular Weight: 2331.64 g/mol
Molecular Formula: C100H179N21O41
Number of labile protons in single surfactant: Zero
Hydrophilic segment:
Molecular Weight: 1029.66 g/mol
Molecular Formula: C62H118N5O6
Number of labile protons in single surfactant: Zero
Hydrophobic segment:
Chemical structure without counter ion:

## Slide 10: CV SANS-dilute solutions
IPTS#25413
Experiments completed: January 2022
Solvent | H (vol%) | D (vol%) | H (wt%) | D (wt%)
001 | 0 | 100 | 0.00 | 100
002 | 5 | 95 | 4.8659 | 95.134
003 | 10 | 90 | 9.3118 | 90.688
004 | 15 | 85 | 13.977 | 86.023
005 | 20 | 80 | 18.331 | 81.669
006 | 25 | 75 | 23.376 | 76.624
Sequence | 100% D2O | 95% D2O | 90% D2O | 85% D2O | 80% D2O | 75% D2O
1 | 3.00 | 3.09 | 3.01 | 3.03 | 3.01 | 3.03
3 | 3.01 | 3.10 | 3.06 | 3.04 | 3.07 | 3.01
5 | 3.01 | 3.04 | 3.08 | 3.05 | 3.09 | 3.03
Solvent (v/v)
Polymer conc. (mg/mL)
Sequence | 100% D2O | 95% D2O | 90% D2O | 85% D2O | 80% D2O | 75% D2O
1 | 2.679 | 2.738 | 2.696 | 2.736 | 2.693 | 2.764
3 | 2.681 | 2.732 | 2.715 | 2.724 | 2.750 | 2.718
5 | 2.696 | 2.692 | 2.742 | 2.756 | 2.777 | 2.740
Polymer conc. (mg/g)